| 161Thorn Hill Road Warrendale, PA 15086-7527 | Audit criteria | AC7117/2 REV. A |
| --- | --- | --- |
|  |  | Issued 2006-11 Revised 2014-09 Superseding AC7117/2 |
| TO BE USED ON AUDITS STARTING ON OR AFTER JANUARY 18, 2015 Nadcap AUDIT CRITERIA FOR AUTOMATED PEENING |
| Editorial Change made to 8.2 on October 15, 2015 |

KEY: Font = Arial 11 pt.; Paragraph Spacing = Before: 12 pt. After: 0 pt.

|  | SCOPE |  |
| --- | --- | --- |
|  | This audit criterion is used to survey a facility seeking Nadcap accreditation for the automated shot peening method. This process method checklist shall be used in conjunction with AC7117. |  |
|  | GENERAL INSTRUCTIONS |  |
|  | See AC7117 Section 2. |  |
|  | Subscriber specific supplements | section na |
|  | Instructions for the Auditors |  |
|  | In completing the prime specific assessment, Auditors are instructed to respond with a “YES” or “NO” to address compliance with each statement or requirement. For any negative responses, the Auditor must clearly indicate if the “NO” reflects noncompliance with respect to existence, adequacy, and/or compliance. Existence relates to documented procedure or policy, and compliance relates to evidence of effective implementation. The “NA” option is used only when the question is not applicable to the Supplier process. Choosing the “NA” option requires an explanation note. |  |  |  |
|  | The Auditor shall apply the questions in the supplemental checklist only to the Suppliers who specify the Customer end-users in the audit scope selection herein. |  |  |  |

| U0 – User Unknown | U8 – Airbus |
| --- | --- |
| U10 – GE Aviation | U11 – The Boeing Company |
| U00 – None |  |

|  | U8 – Airbus Supplement | section na |
| --- | --- | --- |
|  | Note: If no automated shot peening is performed for Airbus check the box to collapse the U8 section. |  |
|  | (U8) Where the arc height is outside the required range/tolerance, do procedures describe appropriate actions to identify the cause and take corrective action? | yes | no |  |
|  | (U8) Do procedures require re-verification of intensity after a significant change in the process? | yes | no |  |
|  | (U8) Is peening equipment either: Fitted with separators and classifiers; Without classifiers but which are fitted with separators which remove fines and it can be demonstrated that there is minimal risk of non-conformance immediately prior to the next scheduled re-assessment and/or shot replacement interval; or Without classifiers and/or separators and with specific written authorization by Airbus? | yes | no |  |
|  | (U8) Is new steel shot conditioned before use? | yes | no |  |
|  | (U8) Does the Supplier have a procedure for shot additions? | yes | no |  |
|  | (U8) Does the Supplier’s procedure ensure that coverage does not exceed 500%? | yes | no |  |
|  | U10 – GE Aviation Supplement | section na |
|  | Note: If no automated shot peening is performed for GE Aviation check the box to collapse the U10 section. |  |  |  |
|  | (U10) Do the Supplier’s procedures prevent the use of centrifugal wheel and manual peening for GE Aviation parts? | yes | no |  |
|  | (U10) Does the Supplier’s equipment, used for P11TF3 peening, include the required hardware interlock or alarm controls that protect against unintended or lack of intended motion? | yes | no |  |
|  | (U10) If required, does the Supplier have a coverage map for the part and do the peened parts meet the coverage map? | yes | no | na |
|  | (U10) Are GE Aviation parts being peened during the automated job audit(s), on a shot peen machine that does not use centrifugal wheel peening? | yes | no | NA |
|  | (U10) Do the Supplier’s procedures verify if there is a requirement of coverage maps for GE Aviation? | yes | no | na |
|  | (U10) Has the Almen saturation curve(s) for GE Aviation parts being peened during the automated job audit(s), been re-run within the previous twelve months? | yes | no | na |

|  | U11 – The Boeing Company Supplement | section na |
| --- | --- | --- |
|  | Note: If no automated shot peening is performed for The Boeing Company check the box to collapse the U11 section. |  |  |  |
|  | (U11) Does the Supplier use only automated equipment to shot peen wing skins, chords, stringers and parts with flat contoured surface areas that are greater than 2 square feet, unless otherwise identified in the engineering drawing? | yes | no | na |
|  | (U11) Does the Supplier use Cast Steel shot that has a hardness of HRC 42-52 when required? | yes | no | na |
|  | (U11) Are the Supplier’s controlled centrifugal force equipment (rotating table type) approved by The Boeing Company prior to use for BAC 5730 PSD 9-7 parts? | yes | no | na |
|  | (U11) Does the Supplier verify that sharp edges and corners are radiused prior to peening to meet the requirements of applicable The Boeing Company specifications? | yes | no |  |
|  | (U11) Does the Supplier verify the peening coverage requirement on a part by visual examination in conjunction with optical examination in accordance with BAC 5730? | yes | no |  |
|  | (U11) Does the amount of material removed post shot peening from low alloy parts (200ksi and above) meet the requirements of The Boeing Company specifications when applicable? | yes | no | na |
|  | (U11) Does the Supplier have evidence of inspection for bulging or rollover condition on parts after peening, as required by BAC 5730? | yes | no |  |
|  | (U11) Does the Supplier have and are they following procedure to visually inspect carburized and hardened The Boeing Company Helicopter parts for damage and notify The Boeing Company Helicopter Material Department when damage is detected, prior to any further processing? | yes | no | na |
|  | (U11) Does the Supplier use distilled water in the wet glass slurry medium? | yes | no | na |
|  | (U11) Are the Supplier’s personnel that are performing or inspecting shot peening operations certified as required in BSS 7630 Table I? | yes | no |  |
|  | (U11) Does the certification training for the Supplier’s shot peening operators meet the requirements of BSS 7630 Sec.5? | yes | no |  |
|  | (U11) Does the re-certification interval meet The Boeing Company requirements of twelve months? | yes | no |  |
|  | EQUIPMENT |  |
|  | General |  |

|  | Does peening equipment have the capability of mechanically moving the shot stream and/or the workpiece? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Does the integral screening equipment classify 100% of the media prior to returning the media to the nozzle? | yes | no | na |
|  | Is the slurry volume of beads maintained per applicable Customer specifications during wet glass peening? | yes | no | na |
|  | ALMEN |  |
|  | No additional audit criteria. |  |
|  | MEDIA |  |
|  | No additional audit criteria. |  |
|  | PERSONNEL |  |
|  | No additional audit criteria. |  |
|  | GENERAL PROCEDURES |  |
|  | Records |  |
|  | Does the Supplier have written procedures to ensure the identity of the specific operator; time, date of start and completion is recorded and retrievable? | yes | no |  |
|  | Software Quality Assurance | section na |
|  | For the purpose of this check sheet, “software” is intended to only cover part-specific process control software (e.g. NC Programs). |  |  |  |
|  | This section applies to Suppliers and processes where the approved process controls are based, at least partially, on a stored and retrieved program or program listing. Typically, these programs are loaded and executed on the peening machine. |  |  |  |
|  | Is there a written procedure for the control of software? | yes | no |  |
|  | Is each program uniquely identified? | yes | no |  |
|  | Is there a revision history maintained of changes to a program? | yes | no |  |
|  | Is the program revision identified in the router or operation sheet/work instruction to allow operator to verify against the control header? | yes | no |  |
|  | Is there an approval process for new and modified programs? | yes | no |  |
|  | Is new or changed program validation (1st piece) approved by quality and records maintained in accordance with the Suppliers quality system and Customer requirements? | yes | no |  |

|  | Are the storage requirements for software programs used to control and monitor the product defined and preserved in a way to prevent loss? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Is there a system in place to prevent unauthorized changes to a program after first piece inspection has been completed and approved? | yes | no |  |
|  | Is there a system in place to prevent access to obsolete software? | yes | no |  |

|  | JOB AUDIT #1 |  |
| --- | --- | --- |
|  | Job Information |  |
|  | A Supplier who has computerized peening equipment may choose to be audited to the automated peening checklist, provided that their Customers do not require computerized peening. Jobs should be chosen according to the NMSE Job Audit Selection Guideline. |  |  |  |
|  | Complete the following and then check the Supplier’s information (technique sheets, travelers) against the purchasing requirements. |  |  |  |
|  | Job Identity/Number: | _______________ |
|  | Technique ID: | _______________ |
|  | Generic Part Description: | _______________ |
|  | Part Number and Revision level (if applicable): | _______________ |
|  | Immediate Customer: | _______________ |
|  | End User (Prime) (If known): | _______________ |
|  | Purchase Order/Revision Level: | _______________ |
|  | Part Quantity: | _______________ |
|  | Serial/Lot Numbers (if provided): | _______________ |
|  | Start Date of Job: | _______________ |
|  | Processing Specification and Revision Level: | _______________ |
|  | Special Purchase Order Requirements: | _______________ |
|  | Is the job audit part live production, demonstration or previously processed? | _______________ |
|  | What Export Control Status did the Supplier identify the part as being? | _______________ |
|  | What status did the Auditor(s) identify themselves as being in the opening meeting? (Restricted or Unrestricted) | _______________ |
|  | Customer Requirements |  |
|  | Are the engineering requirements provided from the purchase order, or in a variety of other forms, flowed down to the shop? | yes | no |  |

|  | Are media size and type flowed down to the shop floor? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Are intensity and strip type flowed down to the shop floor? | yes | no |  |
|  | Are peening required areas, optional areas, and/or prohibited areas flowed down to the shop floor? | yes | no |  |
|  | Is the amount of part coverage flowed down to the shop floor? | yes | no | na |
|  | Implementation of Supplier Procedures |  |  |  |
|  | Is the peening operation at this facility performed in the correct sequence as allowed by the traveler? | yes | no |  |
|  | Have the required Customer approval(s) been obtained for the current technique sheet? | yes | no | na |
|  | Are all operations, inspections, and tests performed prior to peening recorded on the traveler or electronic form, stamped, signed, or initialed and including date? | yes | no |  |
|  | If there are changes in travelers and/or technique sheets, are they approved and dated by authorized personnel? | yes | no | na |
|  | Do the personnel who are performing computerized peening operations and final inspections have the required training and qualification? | yes | no |  |
|  | Do all gages used to measure parameters in the technique sheet have current calibration identification? | yes | no |  |
|  | Are gages that are not calibrated labeled as “reference only” or similarly marked? | yes | no | na |
|  | Are Almen, part holding, masking, and nozzle fixtures compliant to applicable specifications? | yes | no |  |
|  | Is the operator capable of identifying equipment malfunctions? | yes | no |  |
|  | Does the operator know how to proceed when there is an equipment malfunction or automatic shut down? | yes | no |  |
|  | Pre-Processing |  |  |  |
|  | Does the Supplier visually inspect the area to be peened for the absence of sharp edges, corrosion, contamination or damage prior to peening and were appropriate actions taken? | yes | no |  |
|  | Do the pre-peening cleaning methods used conform to the Customer requirements? | yes | no | na |
|  | During the job audit, the Auditor shall witness the following pre-processing tasks. |  |  |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in applying the masking requirements to the parts? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in equipment and fixture usage? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in the use of Almen gage and Almen strip? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in the use of Almen strip fixtures? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in calculating the resultant arc height (if pre-bow compensation method is used)? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in nozzle/wheel position setup? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in understanding saturation curves? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in media sampling which accurately represents the condition of the shot stream media? | yes | no |  |
|  | Processing |  |  |  |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for media type? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for screens? | yes | no | na |
|  | Did in-process media quality inspection meet the Customer requirements for sieve analysis results? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for shape sample inspection area? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for the actual unacceptable shape? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer specified requirements? | yes | no | na |
|  | Are periodic media quality inspections performed at the required intervals? | yes | no |  |
|  | Is the slurry volume of beads maintained per applicable specifications during wet glass peening? | yes | no | na |
|  | Are parts processed in accordance with a technique sheet? | yes | no |  |

|  | Does the technique sheet or traveler document all relevant operations performed by the operator? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Do the Almen fixture locations represent the surfaces to be peened? | yes | no | na |
|  | Does the Almen fixture being used provide the same number, type, location, and orientation of the Almen strips described in the technique sheet? | yes | no |  |
|  | If shaded strips are used, does the Supplier have approval to use them? | yes | no | na |
|  | Technique Sheet and Shop Floor Discipline |  |  |  |
|  | Is the job audit part number specified on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is the job audit technique sheet revision controlled and correctly followed in production? | yes | no |  |
|  | Are job audit part program(s) with revision identified on the technique sheet and being followed in production? | yes | no | na |
|  | Are approvals from both Supplier and Customer on the job audit technique sheet and does the technique sheet have required approvals? | yes | no | na |
|  | Are part specific tooling and fixtures identified on the technique sheet and correctly followed in production? | yes | no |  |
|  | Are Almen fixtures identified on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is part masking identified on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the identification of peening equipment listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is number of nozzles or wheels listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is air pressure or wheel speed listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is nozzle size listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is air jet size listed on the technique sheet and correctly followed in production? | yes | no | na |

|  | Is part rotation or translation rate listed on the technique sheet and correctly followed in production? | yes | no | na |
| --- | --- | --- | --- | --- |
|  | Are setup sketches or photos listed on the technique sheet and is the observed set up in the job audit accurately described? | yes | no |  |
|  | Is nozzle or wheel translation speed listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is travel direction, and travel distance to the part listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is nozzle or wheel position to the part listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the part orientation setup relative to the machine listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is shot flow control listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is shot flow value listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is part peening time (or cycles) listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is almen strip peening time (or cycles) listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is media size, hardness, and type listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is required intensity and test strip type listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is the amount of coverage listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Process Validation |  |  |  |
|  | Does the Supplier process substantiation data include a saturation curve consisting of a minimum of 4 points (not including “0” point) for each intensity determination location? | yes | no |  |
|  | Does the Supplier process substantiation data include intensity verification tests performed at required intervals? | yes | no |  |
|  | Does the Supplier process substantiation data include appropriate actions (e.g. accept/reject) based on the job audit Almen strip readings? | yes | no |  |

|  | Verify the following values for two Almen locations or if applicable a single location at two times for the job audit part. |  |  |  |
| --- | --- | --- | --- | --- |
|  | Are the observed Almen strip locations used to verify the intensity correctly located? | yes | no |  |
|  | Is the observed Almen strip type used to verify the intensity correct? | yes | no |  |
|  | Is the observed intensity value compliant to the Customer intensity requirement? | yes | no |  |
|  | Is the observed intensity verification range compliant to requirements? | yes | no |  |
|  | Is the observed initial Almen reading compliant to requirements? | yes | no |  |
|  | Is the observed final Almen reading compliant to requirements? | yes | no | na |
|  | For one of the job audits, the Auditor shall witness the generation of saturation curve data and media inspections to verify that the following are correct. |  |  |  |
|  | Does the generation of the saturation curve utilize of a minimum of 4 points for each intensity determination location (not including the zero point)? | yes | no |  |
|  | Are the practices of SAE J443 followed? | yes | no |  |
|  | Does the media inspection verify shot size by sieve analysis or wet glass verification by bead slurry concentration? | yes | no |  |
|  | Does the media inspection verify shot fracture counts and shape inspection; or wet glass verification by bead slurry fines concentration? | yes | no |  |
|  | Post Peening Inspection |  |  |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency during the inspection of fluorescent tracer? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency during part inspection for coverage using magnification and other inspection aids? | yes | no |  |
|  | Is final inspection for coverage and effectiveness of applicable masking performed? | yes | no |  |
|  | Is the coverage inspected visually on all parts (100%) or in accordance with an approved sampling plan? | yes | no |  |
|  | (INFO) Record the frequency of inspection: | _______________ |
|  | Are part serial numbers maintained throughout the peening operation? | yes | no | na |

|  | Do the post-peening cleaning methods used conform to the Customer requirements? | yes | no | na |
| --- | --- | --- | --- | --- |
|  | Were parts handled, stored, and transported in a manner to prevent damage? | yes | no |  |
|  | Did final inspection result in the proper disposition of the part(s) audited? | yes | no |  |
|  | Did an inspection check that the part is free from media debris (internal and external), masking residue, edge rollover, and handling damage and were appropriate actions taken? | yes | no |  |
|  | Is the traveler properly completed prior to the part continuing to the next operation or shipment to the Customer? | yes | no |  |
|  | When required, does the certification that is returned to the Customer meet the Customer requirements? | yes | no | na |
|  | (INFO) If YES record the Certification number here: | _______________ |

|  | JOB AUDIT #2 | section na |
| --- | --- | --- |
|  | Job Information |  |
|  | A Supplier who has computerized peening equipment may choose to be audited to the automated peening checklist, provided that their Customers do not require computerized peening. Jobs should be chosen according to the NMSE Job Audit Selection Guideline. |  |  |  |
|  | Complete the following and then check the Supplier’s information (technique sheets, travelers) against the purchasing requirements. |  |  |  |
|  | Job Identity/Number: | _______________ |
|  | Technique ID: | _______________ |
|  | Generic Part Description: | _______________ |
|  | Part Number and Revision level (if applicable): | _______________ |
|  | Immediate Customer: | _______________ |
|  | End User (Prime) (If known): | _______________ |
|  | Purchase Order/Revision Level: | _______________ |
|  | Part Quantity: | _______________ |
|  | Serial/Lot Numbers (if provided): | _______________ |
|  | Start Date of Job: | _______________ |
|  | Processing Specification and Revision Level: | _______________ |
|  | Special Purchase Order Requirements: | _______________ |
|  | Is the job audit part live production, demonstration or previously processed? | _______________ |
|  | What Export Control Status did the Supplier identify the part as being? | _______________ |
|  | What status did the Auditor(s) identify themselves as being in the opening meeting? (Restricted or Unrestricted) | _______________ |
|  | Customer Requirements |  |
|  | Are the engineering requirements provided from the purchase order, or in a variety of other forms, flowed down to the shop? | yes | no |  |
|  | Are media size and type flowed down to the shop floor? | yes | no |  |

|  | Are intensity and strip type flowed down to the shop floor? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Are peening required areas, optional areas, and/or prohibited areas flowed down to the shop floor? | yes | no |  |
|  | Is the amount of part coverage flowed down to the shop floor? | yes | no | na |
|  | Implementation of Supplier Procedures |  |  |  |
|  | Is the peening operation at this facility performed in the correct sequence as allowed by the traveler? | yes | no |  |
|  | Have the required Customer approval(s) been obtained for the current technique sheet? | yes | no | na |
|  | Are all operations, inspections, and tests performed prior to peening recorded on the traveler or electronic form, stamped, signed, or initialed and including date? | yes | no |  |
|  | If there are changes in travelers and/or technique sheets, are they approved and dated by authorized personnel? | yes | no | na |
|  | Do the personnel who are performing computerized peening operations and final inspections have the required training and qualification? | yes | no |  |
|  | Do all gages used to measure parameters in the technique sheet have current calibration identification? | yes | no |  |
|  | Are gages that are not calibrated labeled as “reference only” or similarly marked? | yes | no | na |
|  | Are Almen, part holding, masking, and nozzle fixtures compliant to applicable specifications? | yes | no |  |
|  | Is the operator capable of identifying equipment malfunctions? | yes | no |  |
|  | Does the operator know how to proceed when there is an equipment malfunction or automatic shut down? | yes | no |  |
|  | Pre-Processing |  |  |  |
|  | Does the Supplier visually inspect the area to be peened for the absence of sharp edges, corrosion, contamination or damage prior to peening and were appropriate actions taken? | yes | no |  |
|  | Do the pre-peening cleaning methods used conform to the Customer requirements? | yes | no | na |
|  | During the job audit, the Auditor shall witness the following pre-processing tasks. |  |  |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in applying the masking requirements to the parts? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in equipment and fixture usage? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in the use of Almen gage and Almen strip? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in the use of Almen strip fixtures? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in calculating the resultant arc height (if pre-bow compensation method is used)? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in nozzle/wheel position setup? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in understanding saturation curves? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in media sampling which accurately represents the condition of the shot stream media? | yes | no |  |
|  | Processing |  |  |  |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for media type? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for screens? | yes | no | na |
|  | Did in-process media quality inspection meet the Customer requirements for sieve analysis results? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for shape sample inspection area? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for the actual unacceptable shape? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer specified requirements? | yes | no | na |
|  | Are periodic media quality inspections performed at the required intervals? | yes | no |  |
|  | Is the slurry volume of beads maintained per applicable specifications during wet glass peening? | yes | no | na |
|  | Are parts processed in accordance with a technique sheet? | yes | no |  |
|  | Does the technique sheet or traveler document all relevant operations performed by the operator? | yes | no |  |

|  | Do the Almen fixture locations represent the surfaces to be peened? | yes | no | na |
| --- | --- | --- | --- | --- |
|  | Does the Almen fixture being used provide the same number, type, location, and orientation of the Almen strips described in the technique sheet? | yes | no |  |
|  | If shaded strips are used, does the Supplier have approval to use them? | yes | no | na |
|  | Technique Sheet and Shop Floor Discipline |  |  |  |
|  | Is the job audit part number specified on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is the job audit technique sheet revision controlled and correctly followed in production? | yes | no |  |
|  | Are job audit part program(s) with revision identified on the technique sheet and being followed in production? | yes | no | na |
|  | Are approvals from both Supplier and Customer on the job audit technique sheet and does the technique sheet have required approvals? | yes | no | na |
|  | Are part specific tooling and fixtures identified on the technique sheet and correctly followed in production? | yes | no |  |
|  | Are Almen fixtures identified on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is part masking identified on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the identification of peening equipment listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is number of nozzles or wheels listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is air pressure or wheel speed listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is nozzle size listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is air jet size listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is part rotation or translation rate listed on the technique sheet and correctly followed in production? | yes | no | na |

|  | Are setup sketches or photos listed on the technique sheet and is the observed set up in the job audit accurately described? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Is nozzle or wheel translation speed listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is travel direction, and travel distance to the part listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is nozzle or wheel position to the part listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the part orientation setup relative to the machine listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is shot flow control listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is shot flow value listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is part peening time (or cycles) listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is almen strip peening time (or cycles) listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is media size, hardness, and type listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is required intensity and test strip type listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is the amount of coverage listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Process Validation |  |  |  |
|  | Does the Supplier process substantiation data include a saturation curve consisting of a minimum of 4 points (not including “0” point) for each intensity determination location? | yes | no |  |
|  | Does the Supplier process substantiation data include intensity verification tests performed at required intervals? | yes | no |  |
|  | Does the Supplier process substantiation data include appropriate actions (e.g. accept/reject) based on the job audit Almen strip readings? | yes | no |  |
|  | Verify the following values for two Almen locations or if applicable a single location at two times for the job audit part. |  |  |  |

|  | Are the observed Almen strip locations used to verify the intensity correctly located? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Is the observed Almen strip type used to verify the intensity correct? | yes | no |  |
|  | Is the observed intensity value compliant to the Customer intensity requirement? | yes | no |  |
|  | Is the observed intensity verification range compliant to requirements? | yes | no |  |
|  | Is the observed initial Almen reading compliant to requirements? | yes | no |  |
|  | Is the observed final Almen reading compliant to requirements? | yes | no | na |
|  | For one of the job audits, the Auditor shall witness the generation of saturation curve data and media inspections to verify that the following are correct. |  |  |  |
|  | Does the generation of the saturation curve utilize of a minimum of 4 points for each intensity determination location (not including the zero point)? | yes | no |  |
|  | Are the practices of SAE J443 followed? | yes | no |  |
|  | Does the media inspection verify shot size by sieve analysis or wet glass verification by bead slurry concentration? | yes | no |  |
|  | Does the media inspection verify shot fracture counts and shape inspection; or wet glass verification by bead slurry fines concentration? | yes | no |  |
|  | Post Peening Inspection |  |  |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency during the inspection of fluorescent tracer? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency during part inspection for coverage using magnification and other inspection aids? | yes | no |  |
|  | Is final inspection for coverage and effectiveness of applicable masking performed? | yes | no |  |
|  | Is the coverage inspected visually on all parts (100%) or in accordance with an approved sampling plan? | yes | no |  |
|  | (INFO) Record the frequency of inspection: | _______________ |
|  | Are part serial numbers maintained throughout the peening operation? | yes | no | na |
|  | Do the post-peening cleaning methods used conform to the Customer requirements? | yes | no | na |

|  | Were parts handled, stored, and transported in a manner to prevent damage? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Did final inspection result in the proper disposition of the part(s) audited? | yes | no |  |
|  | Did an inspection check that the part is free from media debris (internal and external), masking residue, edge rollover, and handling damage and were appropriate actions taken? | yes | no |  |
|  | Is the traveler properly completed prior to the part continuing to the next operation or shipment to the Customer? | yes | no |  |
|  | When required, does the certification that is returned to the Customer meet the Customer requirements? | yes | no | na |
|  | (INFO) If YES record the Certification number here: | _______________ |

|  | JOB AUDIT #3 | section na |
| --- | --- | --- |
|  | Job Information |  |
|  | A Supplier who has computerized peening equipment may choose to be audited to the automated peening checklist, provided that their Customers do not require computerized peening. Jobs should be chosen according to the NMSE Job Audit Selection Guideline. |  |  |  |
|  | Complete the following and then check the Supplier’s information (technique sheets, travelers) against the purchasing requirements. |  |  |  |
|  | Job Identity/Number: | _______________ |
|  | Technique ID: | _______________ |
|  | Generic Part Description: | _______________ |
|  | Part Number and Revision level (if applicable): | _______________ |
|  | Immediate Customer: | _______________ |
|  | End User (Prime) (If known): | _______________ |
|  | Purchase Order/Revision Level: | _______________ |
|  | Part Quantity: | _______________ |
|  | Serial/Lot Numbers (if provided): | _______________ |
|  | Start Date of Job: | _______________ |
|  | Processing Specification and Revision Level: | _______________ |
|  | Special Purchase Order Requirements: | _______________ |
|  | Is the job audit part live production, demonstration or previously processed? | _______________ |
|  | What Export Control Status did the Supplier identify the part as being? | _______________ |
|  | What status did the Auditor(s) identify themselves as being in the opening meeting? (Restricted or Unrestricted) | _______________ |
|  | Customer Requirements |  |
|  | Are the engineering requirements provided from the purchase order, or in a variety of other forms, flowed down to the shop? | yes | no |  |
|  | Are media size and type flowed down to the shop floor? | yes | no |  |

|  | Are intensity and strip type flowed down to the shop floor? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Are peening required areas, optional areas, and/or prohibited areas flowed down to the shop floor? | yes | no |  |
|  | Is the amount of part coverage flowed down to the shop floor? | yes | no | na |
|  | Implementation of Supplier Procedures |  |  |  |
|  | Is the peening operation at this facility performed in the correct sequence as allowed by the traveler? | yes | no |  |
|  | Have the required Customer approval(s) been obtained for the current technique sheet? | yes | no | na |
|  | Are all operations, inspections, and tests performed prior to peening recorded on the traveler or electronic form, stamped, signed, or initialed and including date? | yes | no |  |
|  | If there are changes in travelers and/or technique sheets, are they approved and dated by authorized personnel? | yes | no | na |
|  | Do the personnel who are performing computerized peening operations and final inspections have the required training and qualification? | yes | no |  |
|  | Do all gages used to measure parameters in the technique sheet have current calibration identification? | yes | no |  |
|  | Are gages that are not calibrated labeled as “reference only” or similarly marked? | yes | no | na |
|  | Are Almen, part holding, masking, and nozzle fixtures compliant to applicable specifications? | yes | no |  |
|  | Is the operator capable of identifying equipment malfunctions? | yes | no |  |
|  | Does the operator know how to proceed when there is an equipment malfunction or automatic shut down? | yes | no |  |
|  | Pre-Processing |  |  |  |
|  | Does the Supplier visually inspect the area to be peened for the absence of sharp edges, corrosion, contamination or damage prior to peening and were appropriate actions taken? | yes | no |  |
|  | Do the pre-peening cleaning methods used conform to the Customer requirements? | yes | no | na |
|  | During the job audit, the Auditor shall witness the following pre-processing tasks. |  |  |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in applying the masking requirements to the parts? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in equipment and fixture usage? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in the use of Almen gage and Almen strip? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in the use of Almen strip fixtures? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in calculating the resultant arc height (if pre-bow compensation method is used)? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in nozzle/wheel position setup? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in understanding saturation curves? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in media sampling which accurately represents the condition of the shot stream media? | yes | no |  |
|  | Processing |  |  |  |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for media type? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for screens? | yes | no | na |
|  | Did in-process media quality inspection meet the Customer requirements for sieve analysis results? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for shape sample inspection area? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer requirements for the actual unacceptable shape? | yes | no | na |
|  | Did in-process media quality inspection results for this job audit meet the Customer specified requirements? | yes | no | na |
|  | Are periodic media quality inspections performed at the required intervals? | yes | no |  |
|  | Is the slurry volume of beads maintained per applicable specifications during wet glass peening? | yes | no | na |
|  | Are parts processed in accordance with a technique sheet? | yes | no |  |
|  | Does the technique sheet or traveler document all relevant operations performed by the operator? | yes | no |  |

|  | Do the Almen fixture locations represent the surfaces to be peened? | yes | no | na |
| --- | --- | --- | --- | --- |
|  | Does the Almen fixture being used provide the same number, type, location, and orientation of the Almen strips described in the technique sheet? | yes | no |  |
|  | If shaded strips are used, does the Supplier have approval to use them? | yes | no | na |
|  | Technique Sheet and Shop Floor Discipline |  |  |  |
|  | Is the job audit part number specified on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is the job audit technique sheet revision controlled and correctly followed in production? | yes | no |  |
|  | Are job audit part program(s) with revision identified on the technique sheet and being followed in production? | yes | no | na |
|  | Are approvals from both Supplier and Customer on the job audit technique sheet and does the technique sheet have required approvals? | yes | no | na |
|  | Are part specific tooling and fixtures identified on the technique sheet and correctly followed in production? | yes | no |  |
|  | Are Almen fixtures identified on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is part masking identified on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the identification of peening equipment listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is number of nozzles or wheels listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is air pressure or wheel speed listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is nozzle size listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is air jet size listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is part rotation or translation rate listed on the technique sheet and correctly followed in production? | yes | no | na |

|  | Are setup sketches or photos listed on the technique sheet and is the observed set up in the job audit accurately described? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Is nozzle or wheel translation speed listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is travel direction, and travel distance to the part listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is nozzle or wheel position to the part listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the part orientation setup relative to the machine listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is shot flow control listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is shot flow value listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is part peening time (or cycles) listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is almen strip peening time (or cycles) listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is media size, hardness, and type listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is required intensity and test strip type listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is the amount of coverage listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Process Validation |  |  |  |
|  | Does the Supplier process substantiation data include a saturation curve consisting of a minimum of 4 points (not including “0” point) for each intensity determination location? | yes | no |  |
|  | Does the Supplier process substantiation data include intensity verification tests performed at required intervals? | yes | no |  |
|  | Does the Supplier process substantiation data include appropriate actions (e.g. accept/reject) based on the job audit Almen strip readings? | yes | no |  |
|  | Verify the following values for two Almen locations or if applicable a single location at two times for the job audit part. |  |  |  |

|  | Are the observed Almen strip locations used to verify the intensity correctly located? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Is the observed Almen strip type used to verify the intensity correct? | yes | no |  |
|  | Is the observed intensity value compliant to the Customer intensity requirement? | yes | no |  |
|  | Is the observed intensity verification range compliant to requirements? | yes | no |  |
|  | Is the observed initial Almen reading compliant to requirements? | yes | no |  |
|  | Is the observed final Almen reading compliant to requirements? | yes | no | na |
|  | For one of the job audits, the Auditor shall witness the generation of saturation curve data and media inspections to verify that the following are correct. |  |  |  |
|  | Does the generation of the saturation curve utilize of a minimum of 4 points for each intensity determination location (not including the zero point)? | yes | no |  |
|  | Are the practices of SAE J443 followed? | yes | no |  |
|  | Does the media inspection verify shot size by sieve analysis or wet glass verification by bead slurry concentration? | yes | no |  |
|  | Does the media inspection verify shot fracture counts and shape inspection; or wet glass verification by bead slurry fines concentration? | yes | no |  |
|  | Post Peening Inspection |  |  |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency during the inspection of fluorescent tracer? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency during part inspection for coverage using magnification and other inspection aids? | yes | no |  |
|  | Is final inspection for coverage and effectiveness of applicable masking performed? | yes | no |  |
|  | Is the coverage inspected visually on all parts (100%) or in accordance with an approved sampling plan? | yes | no |  |
|  | (INFO) Record the frequency of inspection: | _______________ |
|  | Are part serial numbers maintained throughout the peening operation? | yes | no | na |
|  | Do the post-peening cleaning methods used conform to the Customer requirements? | yes | no | na |

|  | Were parts handled, stored, and transported in a manner to prevent damage? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Did final inspection result in the proper disposition of the part(s) audited? | yes | no |  |
|  | Did an inspection check that the part is free from media debris (internal and external), masking residue, edge rollover, and handling damage and were appropriate actions taken? | yes | no |  |
|  | Is the traveler properly completed prior to the part continuing to the next operation or shipment to the Customer? | yes | no |  |
|  | When required, does the certification that is returned to the Customer meet the Customer requirements? | yes | no | na |
|  | (INFO) If YES record the Certification number here: | _______________ |

# Text boxes

NOTE THIS IS NOT AN OFFICIAL COPY OF THE CHECKLIST AND IS OFFERED ONLY AS A STARTING POINT FOR THE SUPPLIER TO CREATE A WORKING SELF-AUDIT TOOL.  BY ACCEPTING AND USING THIS DOCUMENT, THE SUPPLIER ACCEPTS ALL RESPONSIBILITY TO ASSURE THE INFORMATION ENCLOSED IS THE SAME AS THE OFFICIAL CHECKLIST AND ITS SUBSEQUENT REVISIONS.