| 161Thorn Hill Road Warrendale, PA 15086-7527 | Audit criteria | AC7117/3 REV. A |
| --- | --- | --- |
|  |  | Issued 2006-11 Revised 2014-09 Superseding AC7117/3 |
| TO BE USED ON AUDITS STARTING ON OR AFTER JANUARY 18, 2015 Nadcap AUDIT CRITERIA FOR PEEN FORMING |
| Editorial Change made to 8.2 on October 15, 2015 |

KEY: Font = Arial 11 pt.; Paragraph Spacing = Before: 12 pt. After: 0 pt.

|  | SCOPE |  |
| --- | --- | --- |
|  | This audit criterion is used to survey a facility seeking Nadcap accreditation for the peen forming method. This process method checklist shall be used in conjunction with AC7117. |  |  |  |
|  | GENERAL INSTRUCTIONS |  |
|  | See AC7117 Section 2. |  |
|  | subscriber specific supplements | section na |
|  | Instructions for the Auditors |  |
|  | In completing the prime specific assessment, Auditors are instructed to respond with a “YES” or “NO” to address compliance with each statement or requirement. For any negative responses, the Auditor must clearly indicate if the “NO” reflects noncompliance with respect to existence, adequacy, and/or compliance. Existence relates to documented procedure or policy, and compliance relates to evidence of effective implementation. The “NA” option is used only when the question is not applicable to the Supplier process. Choosing the “NA” option requires an explanation note. |  |  |  |
|  | The Auditor shall apply the questions in the supplemental checklist only to the Suppliers who specify the Customer end-users in the audit scope selection herein. |  |  |  |

| U0 – User Unknown | U8 – Airbus |
| --- | --- |
| U10 – GE Aviation | U11 – The Boeing Company |
| U00 – None |  |

|  | U8 – Airbus Supplement | section na |
| --- | --- | --- |
|  | Note: If no peen forming is performed for Airbus check the box to collapse the U8 section. |  |  |  |
|  | There are no Airbus (U8) supplement questions for Peen Forming. |  |  |  |
|  | U10 – GE Aviation Supplement | section na |
|  | Note: If no peen forming is performed for GE Aviation check the box to collapse the U10 section. |  |  |  |
|  | There are no GE Aviation (U10) supplement questions for Peen Forming. |  |  |  |
|  | U11 – The Boeing Company Supplement | section na |
|  | Note: If no peen forming is performed for The Boeing Company check the box to collapse the U11 section. |  |  |  |
|  | (U11) Does the Supplier have controls to ensure that pre-stressing of parts to be shot peen formed do not exceed the elastic limits of the material as required per applicable specifications? | yes | no | na |
|  | NA only for parts that are not pre-stressed. |  |  |  |
|  | (U11) Does the Supplier verify that sharp edges are radiused prior to peen forming? | yes | no |  |
|  | (U11) Are shot peen formed parts inspected for rollover and bulging? | yes | no |  |
|  | (U11) Is surface roughness being measured after peen forming to meet the drawing requirements? | yes | no | na |
|  | EQUIPMENT |  |
|  | No additional audit criteria. |  |  |  |
|  | ALMEN |  |
|  | No additional audit criteria. |  |
|  | MEDIA |  |
|  | When large or nonstandard peening media are used for peen forming applications, do they meet applicable specification? | yes | no | na |
|  | PERSONNEL |  |
|  | Operator Qualification |  |
|  | Does the Supplier have a documented procedure which prevents an unqualified operator to perform peen forming? | yes | no |  |
|  | GENERAL PROCEDURES |  |
|  | Records |  |

|  | Does the Supplier have written procedures to ensure the identity of the specific operator; time, date of start and completion is recorded and retrievable? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | When manual peening is used for peen forming, are there Supplier procedures that control whether the use complies with the Customer requirements? | yes | no | na |
|  | Software Quality Assurance | section na |
|  | For the purpose of this check sheet, “software” is intended to only cover part-specific process control software (e.g. NC Programs). |  |  |  |
|  | This section applies to Suppliers and processes where the approved process controls are based, at least partially, on a stored and retrieved program or program listing. Typically, these programs are loaded and executed on the peening machine. |  |  |  |
|  | Is there a written procedure for the control of software? | yes | no |  |
|  | Is each program uniquely identified? | yes | no |  |
|  | Is there a revision history maintained of changes to a program? | yes | no |  |
|  | Is the program revision identified in the router or operation sheet/work instruction to allow operator to verify against the control header? | yes | no |  |
|  | Is there an approval process for new and modified programs? | yes | no |  |
|  | Is new or changed program validation (1st piece) approved by quality and records maintained in accordance with the Suppliers quality system and Customer requirements? | yes | no |  |
|  | Are the storage requirements for software programs used to control and monitor the product defined and preserved in a way to prevent loss? | yes | no |  |
|  | Is there a system in place to prevent unauthorized changes to a program after first piece inspection has been completed and approved? | yes | no |  |
|  | Is there a system in place to prevent access to obsolete software? | yes | no |  |
|  | Internal Procedures |  |  |  |
|  | When pre-stress peening is used for forming, are there Supplier procedures that control the use and compliance with Prime requirements? | yes | no | na |
|  | When surface finish is measured after peen forming, is there Supplier procedures that control the methods and equipment used to measure surface finish? | yes | no | na |

|  | When surface finish is improved after peen forming, is there Supplier procedures that control the methods used to improve the surface finish? (e.g. sanding, buffing, etc.) | yes | no | na |
| --- | --- | --- | --- | --- |

|  | JOB AUDIT #1 |  |
| --- | --- | --- |
|  | Job Information |  |
|  | Since peen forming jobs are frequently performed in combination with compression peening using one of the other AC7117 methods (e.g. Automated peening), it is recommended that the same part peening jobs be audited for this job and the associated peening method. |  |  |  |
|  | Complete the following and then check the Supplier’s information (technique sheets, travelers) against the purchasing requirements. |  |  |  |
|  | Job Identity/Number: | _______________ |
|  | Technique ID: | _______________ |
|  | Generic Part Description: | ______________ |
|  | Part Number and Revision level (if applicable): | ______________ |
|  | Immediate Customer: | ______________ |
|  | End User (Prime) (If known): | ______________ |
|  | Purchase Order/Revision Level: | ______________ |
|  | Part Quantity: | ______________ |
|  | Serial/Lot Numbers (if provided): | ______________ |
|  | Start Date of Job: | ______________ |
|  | Processing Specification and Revision Level: | ______________ |
|  | Special Purchase Order Requirements: | ______________ |
|  | Is the job audit part live production, demonstration or previously processed? | ______________ |
|  | What Export Control Status did the Supplier identify the part as being? | ______________ |
|  | What status did the Auditor(s) identify themselves as being in the opening meeting? (Restricted or Unrestricted) | ______________ |
|  | If this job audit is done in combination with another peening method job audit, record the other job number reference here. | ______________ |
|  | Customer Requirements |  |  |  |
|  | Are the engineering requirements provided from the purchase order, or in a variety of other forms, flowed down to the shop? | yes | no |  |

|  | Are media size and type flowed down to the shop floor? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Are intensity and strip type flowed down to the shop floor? | yes | no | na |
|  | Are peening required areas, optional areas, and/or prohibited areas flowed down to the shop floor? | yes | no |  |
|  | Is the amount of part coverage flowed down to the shop floor? | yes | no | na |
|  | Is pre-peen dimensional controls (e.g. fit tolerance), flowed down to the shop floor? | yes | no |  |
|  | Are post-peen dimensional controls areas flowed down to the shop floor? | yes | no |  |
|  | Implementation of Supplier Procedures |  |  |  |
|  | Is the peening operation at this facility performed in the correct sequence as allowed by the traveler? | yes | no |  |
|  | Have the required Customer approval(s) been obtained for the current technique sheet? | yes | no | na |
|  | Are all operations, inspections, and tests performed prior to peening recorded on the traveler or electronic form, stamped, signed, or initialed and including date? | yes | no |  |
|  | If there are changes in travelers and/or technique sheets, are they approved and dated by authorized personnel? | yes | no | na |
|  | Do the personnel, who are performing peen forming, and/or saturation peening operations, and final inspections have the required training and qualification? | yes | no |  |
|  | Do all gages used to measure parameters in the technique sheet have current calibration identification? | yes | no |  |
|  | Are gages that are not calibrated labeled as “reference only” or similarly marked? | yes | no | na |
|  | Are Almen, part holding, masking, and nozzle fixtures compliant to applicable specifications? | yes | no |  |
|  | Is the operator capable of identifying equipment malfunctions? | yes | no |  |
|  | Does the operator know how to proceed when there is an equipment malfunction or automatic shut down? | yes | no |  |
|  | Pre-Processing |  |  |  |
|  | Does the Supplier visually inspect the area to be peened for the absence of sharp edges, corrosion, contamination or damage prior to peening and were appropriate actions taken? | yes | no |  |
|  | Do the pre-peening cleaning methods used conform to the Customer requirements? | yes | no | na |
|  | During the job audit, the Auditor shall witness the following pre-processing tasks. |  |  |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in applying the masking requirements to the parts? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in equipment usage and fixture usage? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in the use of Almen gage and Almen strip? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in the use of Almen strip fixtures? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in calculating the resultant arc height (if pre-bow compensation method is used)? | yes | no | na |
|  | Are periodic media quality inspections performed at the required intervals? | yes | no |  |
|  | Processing |  |  |  |
|  | Are parts processed in accordance with a technique sheet? | yes | no |  |
|  | Does the technique sheet document all relevant operations performed by the operator? | yes | no |  |
|  | Do the Almen fixture locations represent the surfaces to be peened? | yes | no | na |
|  | When used, does the Almen fixture being used provide the same number, type, location, and orientation of the Almen strips described in the technique sheet? | yes | no | na |
|  | Technique Sheet and Shop Floor Discipline |  |  |  |
|  | Is the job audit part number specified on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is the job audit technique sheet revision controlled and correctly followed in production? | yes | no |  |
|  | Are job audit part program(s) with revision identified on the technique sheet and being followed in production? | yes | no | na |
|  | Are approvals from both Supplier and Customer on the job audit technique sheet and does the technique sheet have required approvals? | yes | no | na |

|  | Are part specific tooling and fixtures identified on the technique sheet and correctly followed in production? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Are Almen fixtures identified on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is part masking identified on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the identification of peening equipment listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is number of nozzles or wheels listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is air pressure or wheel speed listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is nozzle size listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is air jet size listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is part rotation or translation rate listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Are setup sketches or photos listed on the technique sheet and is the observed set up in the job audit accurately described? | yes | no |  |
|  | Is nozzle or wheel translation speed listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is travel direction, and travel distance to the part listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is nozzle or wheel position to the part listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the part orientation setup relative to the machine listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is shot flow control listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is shot flow value listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is part peening time (or cycles) listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is Almen strip peening time (or cycles) listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is media size, hardness, and type listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is required intensity and test strip type listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the amount of coverage listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | When compression peening is performed with peen forming, is the minimum intensity of the compression peening met? | yes | no | na |
|  | Process Validation |  |  |  |
|  | Does the Supplier process substantiation data include a saturation curve consisting of a minimum of 4 points (not including “0” point) for each intensity determination location? | yes | no | na |
|  | Does the Supplier process substantiation data include intensity verification tests performed at required intervals? | yes | no | na |
|  | Does the Supplier process substantiation data include appropriate actions (e.g. accept/reject) based on the job audit Almen strip readings? | yes | no | na |
|  | Verify the following values for two Almen locations or if applicable a single location at two times for the job audit part. |  |  |  |
|  | Are the observed Almen strip locations used to verify the intensity correctly located? | yes | no | na |
|  | Is the observed Almen strip type used to verify the intensity correct? | yes | no | na |
|  | Is the observed intensity value compliant to the Customer intensity requirement? | yes | no | na |
|  | Is the observed intensity verification range compliant to requirements? | yes | no | na |
|  | Is the observed initial Almen reading compliant to requirements? | yes | no | na |
|  | Is the observed intermediate Almen reading compliant to requirements? | yes | no | na |
|  | Is the observed final Almen reading compliant to requirements? | yes | no | na |
|  | For one of the job audits, the Auditor shall witness the generation of saturation curve data and media inspections to verify that the following are correct. |  |  |  |
|  | Does the generation of the saturation curve utilize of a minimum of 4 points for each intensity determination location (not including the zero point)? | yes | no | na |
|  | Are the practices of SAE J443 followed? | yes | no | na |
|  | Does the media inspection verify shot size by sieve analysis? | yes | no |  |
|  | Does the media inspection verify shot fracture counts and shape inspection? | yes | no |  |
|  | Post Peening Inspection |  |  |  |
|  | When required, did the operator and/or appropriate personnel demonstrate proficiency during the inspection of fluorescent tracer? | yes | no | na |
|  | When required, did the operator and/or appropriate personnel demonstrate proficiency during part inspection for coverage using magnification and other inspection aids? | yes | no | na |
|  | When required, is final inspection for coverage and effectiveness of applicable masking performed? | yes | no | na |
|  | When compression peening is performed with peen forming, is complete compression peening coverage controlled in the required areas? | yes | no | na |
|  | Are part serial numbers maintained throughout the peening operation? | yes | no | na |
|  | Do the post-peening cleaning methods used conform to the Customer requirements? | yes | no | na |
|  | Were parts handled, stored, and transported in a manner to prevent damage? | yes | no |  |
|  | Did final inspection result in the proper disposition of the part(s) audited? | yes | no |  |
|  | Did an inspection check that the part is free from media debris (internal and external), masking residue, edge rollover, and handling damage and were appropriate actions taken? | yes | no |  |
|  | Is the traveler properly completed prior to the part continuing to the next operation or shipment to the Customer? | yes | no |  |
|  | When required, does the certification that is returned to the Customer meet the Customer requirements? | yes | no | na |
|  | (INFO) If YES record the Certification number here: | _______________ |

|  | JOB AUDIT #2 | section na |
| --- | --- | --- |
|  | Job Information |  |
|  | Since peen forming jobs are frequently performed in combination with compression peening using one of the other AC7117 methods (e.g. Automated peening), it is recommended that the same part peening jobs be audited for this job and the associated peening method. |  |  |  |
|  | Complete the following and then check the Supplier’s information (technique sheets, travelers) against the purchasing requirements. |  |  |  |
|  | Job Identity/Number: | _______________ |
|  | Technique ID: | _______________ |
|  | Generic Part Description: | ______________ |
|  | Part Number and Revision level (if applicable): | ______________ |
|  | Immediate Customer: | ______________ |
|  | End User (Prime) (If known): | ______________ |
|  | Purchase Order/Revision Level: | ______________ |
|  | Part Quantity: | ______________ |
|  | Serial/Lot Numbers (if provided): | ______________ |
|  | Start Date of Job: | ______________ |
|  | Processing Specification and Revision Level: | ______________ |
|  | Special Purchase Order Requirements: | ______________ |
|  | Is the job audit part live production, demonstration or previously processed? | ______________ |
|  | What Export Control Status did the Supplier identify the part as being? | ______________ |
|  | What status did the Auditor(s) identify themselves as being in the opening meeting? (Restricted or Unrestricted) | ______________ |
|  | If this job audit is done in combination with another peening method job audit, record the other job number reference here. | ______________ |
|  | Customer Requirements |  |  |  |
|  | Are the engineering requirements provided from the purchase order, or in a variety of other forms, flowed down to the shop? | yes | no |  |

|  | Are media size and type flowed down to the shop floor? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Are intensity and strip type flowed down to the shop floor? | yes | no | na |
|  | Are peening required areas, optional areas, and/or prohibited areas flowed down to the shop floor? | yes | no |  |
|  | Is the amount of part coverage flowed down to the shop floor? | yes | no | na |
|  | Is pre-peen dimensional controls (e.g. fit tolerance), flowed down to the shop floor? | yes | no |  |
|  | Are post-peen dimensional controls areas flowed down to the shop floor? | yes | no |  |
|  | Implementation of Supplier Procedures |  |  |  |
|  | Is the peening operation at this facility performed in the correct sequence as allowed by the traveler? | yes | no |  |
|  | Have the required Customer approval(s) been obtained for the current technique sheet? | yes | no | na |
|  | Are all operations, inspections, and tests performed prior to peening recorded on the traveler or electronic form, stamped, signed, or initialed and including date? | yes | no |  |
|  | If there are changes in travelers and/or technique sheets, are they approved and dated by authorized personnel? | yes | no | na |
|  | Do the personnel, who are performing peen forming, and/or saturation peening operations, and final inspections have the required training and qualification? | yes | no |  |
|  | Do all gages used to measure parameters in the technique sheet have current calibration identification? | yes | no |  |
|  | Are gages that are not calibrated labeled as “reference only” or similarly marked? | yes | no | na |
|  | Are Almen, part holding, masking, and nozzle fixtures compliant to applicable specifications? | yes | no |  |
|  | Is the operator capable of identifying equipment malfunctions? | yes | no |  |
|  | Does the operator know how to proceed when there is an equipment malfunction or automatic shut down? | yes | no |  |
|  | Pre-Processing |  |  |  |
|  | Does the Supplier visually inspect the area to be peened for the absence of sharp edges, corrosion, contamination or damage prior to peening and were appropriate actions taken? | yes | no |  |
|  | Do the pre-peening cleaning methods used conform to the Customer requirements? | yes | no | na |
|  | During the job audit, the Auditor shall witness the following pre-processing tasks. |  |  |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in applying the masking requirements to the parts? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in equipment usage and fixture usage? | yes | no |  |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in the use of Almen gage and Almen strip? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in the use of Almen strip fixtures? | yes | no | na |
|  | Did the operator and/or appropriate personnel demonstrate proficiency in calculating the resultant arc height (if pre-bow compensation method is used)? | yes | no | na |
|  | Are periodic media quality inspections performed at the required intervals? | yes | no |  |
|  | Processing |  |  |  |
|  | Are parts processed in accordance with a technique sheet? | yes | no |  |
|  | Does the technique sheet document all relevant operations performed by the operator? | yes | no |  |
|  | Do the Almen fixture locations represent the surfaces to be peened? | yes | no | na |
|  | When used, does the Almen fixture being used provide the same number, type, location, and orientation of the Almen strips described in the technique sheet? | yes | no | na |
|  | Technique Sheet and Shop Floor Discipline |  |  |  |
|  | Is the job audit part number specified on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is the job audit technique sheet revision controlled and correctly followed in production? | yes | no |  |
|  | Are job audit part program(s) with revision identified on the technique sheet and being followed in production? | yes | no | na |
|  | Are approvals from both Supplier and Customer on the job audit technique sheet and does the technique sheet have required approvals? | yes | no | na |

|  | Are part specific tooling and fixtures identified on the technique sheet and correctly followed in production? | yes | no |  |
| --- | --- | --- | --- | --- |
|  | Are Almen fixtures identified on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is part masking identified on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the identification of peening equipment listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is number of nozzles or wheels listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is air pressure or wheel speed listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is nozzle size listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is air jet size listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is part rotation or translation rate listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Are setup sketches or photos listed on the technique sheet and is the observed set up in the job audit accurately described? | yes | no |  |
|  | Is nozzle or wheel translation speed listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is travel direction, and travel distance to the part listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is nozzle or wheel position to the part listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the part orientation setup relative to the machine listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is shot flow control listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is shot flow value listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is part peening time (or cycles) listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is Almen strip peening time (or cycles) listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is media size, hardness, and type listed on the technique sheet and correctly followed in production? | yes | no |  |
|  | Is required intensity and test strip type listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | Is the amount of coverage listed on the technique sheet and correctly followed in production? | yes | no | na |
|  | When compression peening is performed with peen forming, is the minimum intensity of the compression peening met? | yes | no | na |
|  | Process Validation |  |  |  |
|  | Does the Supplier process substantiation data include a saturation curve consisting of a minimum of 4 points (not including “0” point) for each intensity determination location? | yes | no | na |
|  | Does the Supplier process substantiation data include intensity verification tests performed at required intervals? | yes | no | na |
|  | Does the Supplier process substantiation data include appropriate actions (e.g. accept/reject) based on the job audit Almen strip readings? | yes | no | na |
|  | Verify the following values for two Almen locations or if applicable a single location at two times for the job audit part. |  |  |  |
|  | Are the observed Almen strip locations used to verify the intensity correctly located? | yes | no | na |
|  | Is the observed Almen strip type used to verify the intensity correct? | yes | no | na |
|  | Is the observed intensity value compliant to the Customer intensity requirement? | yes | no | na |
|  | Is the observed intensity verification range compliant to requirements? | yes | no | na |
|  | Is the observed initial Almen reading compliant to requirements? | yes | no | na |
|  | Is the observed intermediate Almen reading compliant to requirements? | yes | no | na |
|  | Is the observed final Almen reading compliant to requirements? | yes | no | na |
|  | For one of the job audits, the Auditor shall witness the generation of saturation curve data and media inspections to verify that the following are correct. |  |  |  |
|  | Does the generation of the saturation curve utilize of a minimum of 4 points for each intensity determination location (not including the zero point)? | yes | no | na |
|  | Are the practices of SAE J443 followed? | yes | no | na |
|  | Does the media inspection verify shot size by sieve analysis? | yes | no |  |
|  | Does the media inspection verify shot fracture counts and shape inspection? | yes | no |  |
|  | Post Peening Inspection |  |  |  |
|  | When required, did the operator and/or appropriate personnel demonstrate proficiency during the inspection of fluorescent tracer? | yes | no | na |
|  | When required, did the operator and/or appropriate personnel demonstrate proficiency during part inspection for coverage using magnification and other inspection aids? | yes | no | na |
|  | When required, is final inspection for coverage and effectiveness of applicable masking performed? | yes | no | na |
|  | When compression peening is performed with peen forming, is complete compression peening coverage controlled in the required areas? | yes | no | na |
|  | Are part serial numbers maintained throughout the peening operation? | yes | no | na |
|  | Do the post-peening cleaning methods used conform to the Customer requirements? | yes | no | na |
|  | Were parts handled, stored, and transported in a manner to prevent damage? | yes | no |  |
|  | Did final inspection result in the proper disposition of the part(s) audited? | yes | no |  |
|  | Did an inspection check that the part is free from media debris (internal and external), masking residue, edge rollover, and handling damage and were appropriate actions taken? | yes | no |  |
|  | Is the traveler properly completed prior to the part continuing to the next operation or shipment to the Customer? | yes | no |  |
|  | When required, does the certification that is returned to the Customer meet the Customer requirements? | yes | no | na |
|  | (INFO) If YES record the Certification number here: | _______________ |

# Text boxes

NOTE THIS IS NOT AN OFFICIAL COPY OF THE CHECKLIST AND IS OFFERED ONLY AS A STARTING POINT FOR THE SUPPLIER TO CREATE A WORKING SELF-AUDIT TOOL.  BY ACCEPTING AND USING THIS DOCUMENT, THE SUPPLIER ACCEPTS ALL RESPONSIBILITY TO ASSURE THE INFORMATION ENCLOSED IS THE SAME AS THE OFFICIAL CHECKLIST AND ITS SUBSEQUENT REVISIONS.